| File Rev. A |  |
| --- | --- |
| Kern Code | Description |  | Build-Up | Color | Conductive |
| A | Cad Plate (Cadmium), per QQ-P-416, Type II Class 3 |  | .0002 – .0003 | Bright Dip | Yes |
| AA | Dull Black Hard Anodize, per Mil-A-8625 Typ. III Class 2 |  | .0015 - .002 | Black |  |
| AB | Dull Black Hard Anodize, per Mil-A-8625 Typ. III Class 2 |  | .0001 - .0004 | Black |  |
| A1 | Aluminum (High purity), per Mil-DTL-83488, Class1 Type II Supplementary chromate treatment shall meet the corrosion resistance requirements of Mil-DTL-5541 Class 1A and the low electrical resistance requirements of Class 3. Electrical resistance shall be less than 2.5 milliohms when tested per EIA-364-83, with contact points being any 2 opposite points on the same shell. |  | .0010 - .0012 |  | Yes |
| B | Cad Plate (Cadmium), per QQ-P-416, Type II Class 3 |  | .0002 – .0003 | Olive Drab | Yes |
| BC | Cad Plate (Cadmium), per QQ-P-416, Type II Class 3 |  | .0002 – .0003 | Black | Yes |
| BD | Gold Iridite, per Mil-C-5541, Class 3 over Cadmium per QQ-P-416, Class 3 |  |  | Gold |  |
| C | Chem Film (Iridite / Alodine), per Mil-C-5541, Class 3 |  |  |  | Yes |
| D | Cad Plate (Cadmium), per QQ-P-416, Type I Class 3 over Electrodeposited Nickel per QQ-N-290, Class 1 Gr. E |  | .0007 - .001 | Bright Dip | Yes |
| E | Cad Plate (Cadmium), per QQ-P-416, Type II Class 3 over Electrodeposited Nickel per QQ-N-290, Class 1 Gr. E |  | .0007 - .001 | Olive Drab | Yes |
| F | Cad Plate (Cadmium), per QQ-P-416, Type I Class 3 over Electroless Nickel per Mil-C26074, Class 3 / 4 Gr. B |  | .0007 - .001 | Bright Dip | Yes |
| G | Cad Plate (Cadmium), per QQ-P-416, Type II Class 3 over Electroless Nickel per Mil-C-26074, Class 3 / 4 Gr. B |  | .0007 - .001 | Olive Drab | Yes |
| GA | Gold, per Mil-G-45204 over Copper (23.5 – 31.5 Micro Inches or 6.8 Microns) |  | 6.8 Microns | Gold |  |
| GB | Gold, per Mil-G-45204 over Copper (51 – 67 Micro Inches or 1.3 – 1.7 Microns) |  | 1.3 – 1.7 Microns | Gold |  |
| H | Electrodeposited Nickel Plate, per QQ-N-290, Class 1 Gr. C |  | .0007 - .001 |  | Yes |
| H1 | Duplex Electrodeposited Nickel: Sulfimate Nickel, per QQ-N-290 Class 1, Category M, .005% Sulfur max., .0006 thick, followed by: Nickle per QQ-N-290 Class 2 .04% Sulfur min., .0004 thick |  | .0010 - .0012 |  | Yes |
| H2 | Teflon Nickel – .0002 - .0004 thick over: Sulfimate Nickel per QQ-N-290 Class 1, Category M, .005% Sulfur max., .0005 thick, followed by: Nickle per QQ-N-290 Class 2 .04% Sulfur min., .0003 thick |  | .0010 - .0012 |  | Yes |
| I | Cad Plate (Cadmium), per Harris Specification |  | .0013 - .0016 |  | Yes |
| J | Electroless Nickel Plate, per SAE AMS-C-26074, Class 3 / 4 (Bake for 1 hr.), Gr. B |  | .0007 - .001 |  | Yes |
| J1 | Duplex Electroless Nickel: Electroless Nickel per ASTM - B733 Class 1 High Phosphorus internal layer Type V (10 -13% P) .0006 thick followed by: Medium Phosphorus external layer Type IV (5 - 8% P) .0004 thick. |  | .0010 - .0012 |  | Yes |
| J2 | Teflon Nickel .0002 - .0004 thick over: Electroless Nickel per ASTM - B733 Class 1 High Phosphorus internal layer Type V (10 -13% P) .0006 thick followed by; Medium Phosphorus external layer Type IV (5 - 8% P) .0004 |  | .0010 - .0012 |  | Yes |
| J3 | Zinc Nickel, in accordance with ASTM - B841 Type D (Dull Black) Grade 10 Shall be Hexavalent Chromate coating over Electroless Nickel per ASTM - B733 Type IV, SC2, Class 5. Post Bake 2 hours @ 350° F. |  | .0010 - .0012 |  | Yes |
| J4 | Black Electrodeposited Nickel, per MIL-P-18317, RoHS |  | .0007 - .0010 | Black | Yes |
| J5 | J3 Zinc Nickel selectively plated over Electroless Nickel per ASTM-B733. Masked per blueprint |  | .0010 - .0012 | Black / Nickel | Yes |
| J6 | Electroless Nickel: per ASTM-B733 Sc3, Type I Class 4 |  | .0016 - .0018 |  | Yes |
| JJ | Electroless Nickel Plate, per SAE AMS-2404, Class 4 |  | .001 - .0013 |  | Yes |
| K | Hard Chrome Plate (Satin Finish), per QQ-C-320 Type II Class 2 |  | .0007 - .001 |  | Yes |
| L | Tin Plate, per Mil-T-10727 Type I |  | .0001 - .00025 | Tin | Yes |
| M | Cad Plate (Gold Iridite), per QQ-P-416 Type II Class 3 over Mil-C-26074B Nickle Strike or QQ-N-290 Nickle Flash |  | .0006 |  | Yes |
| N | Gold Plate, per Mil-G-45204 Type II Class II |  | .0001 - .00015 | Gold | Yes |
| P | Passivate, per ASTM-A967, QQ-P-35 (for CRES parts only) |  |  |  | Yes |
| P1 | Passivate – 303 Stainless Steel per AMS-QQ-P-35 Type II |  |  |  | Yes |
| P2 | Passivate – 304, 316, and 321 Stainless Steel per AMS-QQ-P-35 Type VI or Type VII |  |  |  | Yes |
| Y | Black Oxide, per Mil-C-13924 Class 1: Iron Steel Class 2: Stainless Steel (other than 300 Series) Class 3: Fused Salt Process Class 4: 300 Series Stainless Copper Alloys: per Mil-F-495 |  |  | Black | Yes |
| R | Black Anodize, per Mil-A-8625 Type II Class 2 (Aluminum Only) |  | .0001 - .0004 | Black | No |
| S | Red Anodize, per Mil-A-8625 Type II Class 2 (Aluminum Only) |  | .0001 - .0004 | Red | No |
| SJ | Electroless Nickel Plate, per Mil-C-26074, Class 3 / 4 (No Grade) |  | .0003 - .0006 |  | Yes |
| T | Green Anodize, per Mil-A-8625 Type II Class 2 (Aluminum Only) |  | .0001 - .0004 | Green | No |
| TJ | Electroless Nickel Plate, per SAE AMS-C-26074, Class 3 / 4 (Bake for 1 hr.), Gr. A |  | .001 - .0013 |  | Yes |
| U | Clear Anodic Coating, per Mil-A-8625 Type II Class 1 (Aluminum Only) |  | .0001 - .0004 |  | No |
| V | Hard Anodize, per Mil-A-8625 Type III Class 1 (Aluminum Only) |  | .0018 - .0022 |  | Yes |
| VA | Silver, per ASTM-B-700 or QQ-S-365 201 – 335 Micro Inches (5.1 – 8.5 Microns) |  | 5.1 – 8.5 Microns | Silver | Yes |
| VB | SILVER PLATE, PER ASTM B 700 TYPE 2, GRADE A, CLASS N, .000204 / .000331 IN. THICK (5.1 µM / 8.4 µM) OVER ELECTROLESS NICKEL PER ASTM B733 TYPE 2 (THICKNESS SHALL BE .0001-INCH MAX) (2.54 µM MAX) PHOSPHORUS 1-3% TOTAL THICKNESS .000219 / .000431 IN (5.6 µM / 10.9 µM) |  | .000219 / .000431 in (5.6 µm / 10.9 µm) | Silver | Yes |
| VC | SILVER PLATE, PER ASTM B 700 TYPE 2, GRADE A, CLASS N, .000204 / .000331 IN. THICK (5.1 µM / 8.4 µM) OVER ELECTROLESS NICKEL PER ASTM B733 TYPE 2 (THICKNESS SHALL BE .0001-INCH MAX) (2.54 µM MAX) PHOSPHORUS 1-3% OVER .000015 INCH THK. MIN. COPPER PER MIL-C-14550 (.38 µM) TOTAL THICKNESS .000269 / .000446 IN (6.8 µM / 11.3 µM) |  | .000269 / .000446 in (6.8 µm / 11.3 µm) | Silver | Yes |
| W | Cad Plate (Cadmium), per QQ-P-416, Type II Class 2 over Electroless Nickel per Mil-C-26074, Class 4 Gr. B. Phosphorus content 9 to 12%. Bake for 1 to 1.5 hours @ 250° ± 10° F (to meet 500 hr. Salt Spray Test) |  | .001 - .0013 | Olive Drab | Yes |
| WW | Cad Plate (Cadmium), per QQ-P-416, Type II Class 2 over Electroless Nickel per Mil-C-26074, Class 3 / 4 Gr. B (to meet 1000 hr. Salt Spray Test) |  | TBA | Olive Drab | Yes |
| XX | Un-Plated, (No Allowance for finish) |  |  |  |  |
| Y | Black Oxide, per Mil-C-13924 Class 1: Iron Steel Class 2: Stainless Steel (other than 300 Series) Class 3: Fused Salt Process Class 4: 300 Series Stainless Copper Alloys: per Mil-F-495 |  |  | Black | Yes |
| Z | Special Finish per Customer Specification / Blueprint |  |  |  |  |
| ZC | Black Zinc Cobalt, per ASTM-B840 |  |  | Black |  |
| ZCG | Green Zinc Cobalt, per ASTM-B840 |  |  | Green |  |